GLEASON ETCH PROCEDURE

1. Obtain 3 acid or base resistant containers that are just large enough to completely submerge the areas to be etched.

2. Thoroughly clean parts to remove any oil and/or contaminants. Dry thoroughly.

Solutions Needed:

Solution #1: 5% HNO3 (Nitric Acid) in alcohol

Solution #2: 10% HCl (Hydrochloric Acid) in alcohol

Solution #3: 5% NH4OH (Ammonium Hydroxide) in water

Notes:

1. These solutions are very reactive and should be mixed slowly, adding small quantities of the acid to the alcohol or ammonium hydroxide to the water. Eye protection must be used.

2. It is beneficial to induce a grinding burn on a scrap piece of carburized steel, quenched and tempered steel, depending on the heat treat condition being evaluated, and run through this procedure to ensure that the procedure is being done properly and the microstructures are being properly evaluated

3. Place all samples in Solution #1 (Each bearing component may be etched one at a time if desired).

4. Samples must sit in the solutions for the exact specified times specified below or there will not be enough blackening with Solution #1 or too much removal with Solution #2. In addition, ensure that the bearing raceway of the inner and outer race is fully submerged in the solutions to ensure the entire bearing surface gets etched. After each of the specified times, drain off any excess solution (but do not rinse) and place it in the next solution.

Procedure:

Solution -1 : Time: 4 minutes at room temperature

1. Solution #1 etches the entire sample black.(After 4 minutes, drain off excess solution but do

not rinse)

Solution-2 : Time: 8 minutes at room temperature

1. Solution #2 removes the black coating selectively according to microstructure. The areas that were heavily burned during the grinding operation and resulted in "reformed untempered martensite will appear dark black.

2. The areas that were less severely burned and resulted in tempered martensite will appear dark gray to light black.

3. The unburned areas will have a uniform gray Appearance

(After 8 minutes, drain off excess solution but do not rinse)

Solution-3: Time: 4 minutes at room temperature

1. If too much blackening occurs, try rinsing with water or alcohol after Solution #3.

(After 4 minutes, drain off excess solution and dry with an air hose immediately, and spray with a clear acrylic or coat with oil to prevent rusting)

Note: 5. Once the samples have been Gleason etched, evaluate the sample for any grinding injury.

Example Pics:

Figure 1 –Shows burning indications after grinder burn test by Gleason etch method

Figure 2 –Shows no burning indications after grinder burn test by Gleason etch method.